TECHNICAL DATA

FOLIA ODBLASKOWA IKOLITE PRISMATIC

Soft Monomeric PVC film

Color: white/yellow/red/green/blue Surface: glossy

MATERIAL DETAILS

| PROPERTIES | TEST METHOD | METRIC |
| --- | --- | --- |
| Film thickness | ISO 4591:1992 | 170 micron Monomeric pvc film |
| Surface | / | glossy |
| Adhesive type | / | Solvent polyacrylate,permanent adhesive,transparent |
| Release paper | / | One side coated silicone paper, 90g/sq.m 2.6oz/sq.yd |
| Shelf life | / | Up to 1 year |
| Application temperature | / | Min.+10 |
| Service life by specialist application Under vertical outdoor exposure (normal climate of China) | / | Up to 1 year |
| Available Size | / | 1.24 |

INK PRINTABILITY

| Solvent | Eco-solvent | UV |  |
| --- | --- | --- | --- |